Elba Daylight™

A bold, textured, light-filtering fabric made of polyester with an acrylic coating, providing privacy while softly diffusing natural light. Designed with a color palette that complements its blackout counterpart, Elba Twilight.

| Openness factor | < 1% |
| --- | --- |
| UV blockage | >99% |
| Visible light transmittance Tv | 23% to 39% |
| Solar Reflectance Rs | Up to 57% |
| SHGC % Improvement | Up to 60% |

certifications

Download Certificates: